## Slide 1
CIRAMICS

## Slide 2: Factors that Determine Crystal Structure
1. Relative sizes of ions – Formation of stable structures:
--maximize the # of oppositely charged ion neighbors.
-
-
-
-
+
unstable
-
-
-
-
+
stable
-
-
-
-
+
stable
2. Maintenance of
Charge Neutrality :
--Net charge in ceramic
should be zero.
--Reflected in chemical
formula:
CaF
2
:
Ca
2+
cation
F
-
F
-
anions
+
A
m
X
p
m, p values to achieve charge neutrality

## Slide 3: Atomic Bonding in Ceramics
• Bonding:
-- Can be ionic and/or covalent in character.
-- % ionic character increases with difference in
electronegativity of atoms.
• Degree of ionic character may be large or small:
SiC: small
CaF2: large

## Slide 4: Coordination # and Ionic Radii
• Coordination number increases with
2
r
cation
r
anion
Coord
#
< 0.155
0.155 - 0.225
0.225 - 0.414
0.414 - 0.732
0.732 - 1.0
3
4
6
8
linear
triangular
tetrahedral
octahedral
cubic
ZnS
(zinc blende)
NaCl
(sodium
chloride)
CsCl
(cesium
chloride)
r
cation
r
anion
To form a stable structure, how many anions can surround a cation?

## Slide 5: c03tf03

## Slide 6: Computation of Minimum Cation-Anion Radius Ratio
Determine minimum rcation/ranion for an octahedral site (C.N. = 6)
a = 2ranion
a
Measure the radii (blue and yellow spheres)
Substitute for “a” in the above equation

## Slide 7: Example Problem: Predicting the Crystal Structure of FeO
• On the basis of ionic radii, what crystal structure would you predict for FeO?
• Answer:
based on this ratio,
-- coord # = 6 because
0.414 < 0.550 < 0.732
-- crystal structure is similar to NaCl
Ionic radius (nm)
0.053
0.077
0.069
0.100
0.140
0.181
0.133
Cation
Anion
Al
3+
Fe
2
+
Fe
3+
Ca
2+
O
2-
Cl
-
F
-

## Slide 8: Rock Salt Structure
Same concepts can be applied to ionic solids in general.
Example: NaCl (rock salt) structure
rNa = 0.102 nm
rNa/rCl = 0.564
cations (Na+) prefer octahedral sites
rCl = 0.181 nm

## Slide 9: MgO and FeO
O2- rO = 0.140 nm
Mg2+ rMg = 0.072 nm
rMg/rO = 0.514
cations prefer octahedral sites
So each Mg2+ (or Fe2+) has 6 neighbor oxygen atoms
MgO and FeO also have the NaCl structure

## Slide 10: AX Crystal Structures
Cesium Chloride structure:
 Since 0.732 < 0.939 < 1.0, cubic sites preferred
So each Cs+ has 8 neighbor Cl-
AX–Type Crystal Structures include NaCl, CsCl, and zinc blende

## Slide 11: AX2 Crystal Structures
Calcium Fluorite (CaF2)
Cations in cubic sites
UO2, ThO2, ZrO2, CeO2
Antifluorite structure –
positions of cations and anions reversed
Fluorite structure

## Slide 12: ABX3 Crystal Structures
Perovskite structure
Ex: complex oxide
BaTiO3

## Slide 13: SUMMARY
• Atoms may assemble into crystalline or amorphous structures.
• We can predict the density of a material, provided we know the atomic weight, atomic radius, and crystal geometry (e.g., FCC, BCC, HCP).
• Common metallic crystal structures are FCC, BCC and HCP. Coordination number and atomic packing factor are the same for both FCC and HCP crystal structures.
• Ceramic crystal structures are based on:
-- maintaining charge neutrality
-- cation-anion radii ratios.
• Interatomic bonding in ceramics is ionic and/or covalent.